## Slide 1
Applying Gibbs Minimization to Reactions Between Impurities in CO2
Introduction and Objectives
Experiment
Results
Conclusion
Methods
References
Experiment 2
Conditions
P: 99 bar
T: 25 C
Component
Input
Output
Output
H2S
SO2
O2
H2O
NO2
NO
H2SO4
36
32
90
20
31
-
-
-
0
25
15
28
4
1
-*
-*
0
0
2
0
31
0
12
56
Experiments 1
Conditions
P: 100 bar
T: 25 C
Component
Input
Output
Output
H2S
SO2
O2
H2O
NO2
NO
H2SO4
HNO3
-
-
-
675
72
-
-
-
0
0
0
675
70
4
-*
-*
0
0
0
673
67
2
3.5
0
HNO3
Discussion
Observed from experiments
Experiment 1: no fog observed, no visible acid formation,
visible coupon surface changes.
Experiment 2: fog clearly observed, stronger chemical reactions than Experiment 1
More…
Model Results
Experiment 1: low acid formation; no liquid phase predicted.
Experiment 2: concentrated H2SO4 acid formation; acid-liquid phase predicted.
Experimental
Model
Experimental
Model
Modelled Acid Formation